## Slide 1: Materials for clean energy
Omar Abdelrahman
(Chemical Engineering)
Ashwin Ramasubramaniam
(Mechanical & Industrial Engineering)

## Slide 2: Lesson Plan
Introduction:
  Examples of chemical reactions that are at the forefront of renewable/sustainable energy
  Materials challenges for catalyzing reactions
  Electrochemical approaches
  Computational modeling
Focus topic: Water Electrolysis and PEM Fuel Cell Experiment
  Hands-on experiment with hydrogen fuel cell
Wrap up

## Slide 3: The “Green” dream
Water Electrolysis: 2H2O (l)  2H2 (g)+ O2 (g)
Cathode: 4H+ + 4e-  2H2 (g)
Anode : 2H2O (l)  O2 (g)+ 4H+ + 4e-
Seh et al., Science 355 (2017)
DOI: 10.1126/science.aad4998
Nitrogen Reduction: N2 + 3H2 (g)  2NH3 (g)
Cathode: N2 + 6H+ + 6e-  2NH3 (g)
Anode : 3H2O (l)  3/2 O2 (g)+ 6H+ + 6e-
CO2 Reduction:
Cathode: xCO2 + nH+ + ne-  product + yH2O (g)
Anode: 2H2O (l)  O2 (g)+ 4H+ + 4e-
Common Theme: Electrochemical transformations to produce energy carriers and/or value-added products
Notes: Electrochemical conversion processes that can convert molecules in the atmosphere (e.g., water, carbon dioxide, and nitrogen) into higher-value products (e.g., hydrogen, hydrocarbons, and ammonia) hold promise for a sustainable energy future
Electrocatalysts play a key role in these energy conversion technologies because they increase the rate, efficiency, and selectivity of the chemical transformations involved
Hydrogen gas, for example, is one such key value-added product that is central in chemical transformations and is highly sought after as a clean fuel. Water electrolysis – clean path to green hydrogen
Ammonia is a highly valuable chemical; also considered a good medium for hydrogen storage. Conventional Haber-Bosch energy intensive, high CO2 footprint. H2 usually comes from hydrocarbons – dirty.

## Slide 4: Example: H2 as a Sustainable fuel – Production
Image: www.energy.gov
Compact; higher current density and operating pressure
Less corrosive electrolytes
Pt cathode; Ir/Ir oxide anode
High-cost, short lifetime of membranes
https://www.epfl.ch/labs/lepa/grid2mobility-demonstrator-martigny/key-technologies/alkaline-electrolyser/
Cheaper catalysts (Ni based)
More durable
Corrosive electrolyte
Slow dynamics, low current density
ACIDIC (PEM)
BASIC (AEM)

## Slide 5: Thermodynamic Analysis
Need at least 1.23 V to drive electrolysis
Inefficiencies in practice lead to “overpotential”  should minimize this ~0 V
Maric and Yu
https://www.intechopen.com/chapters/62151

## Slide 6: Example: H2 as a sustainable fuel – Energy production
NIST.gov
PEM Fuel Cell
nafion.com
Recall Water Electrolysis: 2H2O (l)  2H2 (g)+ O2 (g)
Cathode: 4H+ + 4e-  2H2 (g)
Anode : 2H2O (l)  O2 (g)+ 4H+ + 4e-
Hydrogen Oxidation: 2H2O (l)  2H2 (g)+ O2 (g)
Anode: 4H+ + 4e-  2H2 (g)
Cathode : 2H2O (l)  O2 (g)+ 4H+ + 4e-
Running electrolysis in reverse

## Slide 7: Example: H2 as a sustainable fuel – Energy production
PEM Fuel Cell
nafion.com
AEM Fuel Cell
Pt catalyst for both anode and cathode
Pt, Pd, Ir (PGM) catalysts

## Slide 8: Thermodynamic Analysis
nafion.com
Hydrogen Oxidation: H2 (g)+ ½ O2 (g)  H2O (l)
Quantity | H2 | 0.5 O2 | H2O | Change
Enthalpy | 0 | 0 | -285.83 kJ | ΔH = -285.83 kJ
Entropy | 130.68 J/K | 0.5 x 205.14 J/K | 69.91 J/K | TΔS = -48.7 kJ
http://hyperphysics.phy-astr.gsu.edu/hbase/thermo/electrol.html
ΔG = ΔH - TΔS = -285.83 kJ + 48.7 kJ = -237.1 kJ (at 25 oC)
Ideal efficiency = ΔG/ΔH = 0.83 (83%)
Cell voltage = ΔG/2F = 1.23 V; 0.7 V typical due to losses
( 2 moles of e- used to produce 1 mole of H2; F - Faraday constant)
Notes: ΔG is what it takes to drive the reaction or what you can get out of the reaction
ΔH is what is stored in the fuel
So in the electrolysis/fuel cell pair where the enthalpy change is 285.8 kJ, you have to put in 237 kJ of energy to drive electrolysis and the heat from the environment will contribute TΔS=48.7 kJ to help you. Going the other way in the fuel cell, you can get out the 237 kJ as electric energy, but have to dump TΔS = 48.7 kJ to the environment.

## Slide 9: Materials Considerations
Electrocatalysts
Reduce energy barriers for reactions (lower energy cost)
Enhance reaction rates – fast kinetics
Increase desired product selectivity
Good electrical conductors (low resistive losses)
Long-term stability – no degradation (leaching, sintering, etc.)
Inexpensive, earth-abundant
Electrolytes, Membrane Materials, Gas Diffusion Layers (another time…)
Wikipedia
Wikipedia

## Slide 10: Electrocatalysts for H2 production
Sabatier Principle: An ideal catalyst neither binds adsorbates too strongly or too weakly
Catalytic activity increases
Chemical Society Reviews, 43(18), 6555-6569.
Weak binding
Strong binding
“Volcano” plot
H+ + e-  ½ H2
Wikipedia
PGM catalysts, Ir-/Ru-based oxides among the best catalysts. Can they be replaced?

## Slide 11
Desirable physical/chemical properties are only part of the story for materials selection
Can we move towards earth-abundant materials?
Their compounds? (Nitrides, phosphides, sulfides, carbides,…)
Can we afford to test all of these one by one?
Societal considerations?
Supply chains?
Environmental impact?

## Slide 12: Computational (Electro)catalysis
QC – corrections for complex active sites
DFT – reaction thermodynamics and barriers
MD – structure-function relationships, reaction dynamics
Continuum – microkinetic models, reactor models
Designing catalysts in silico
Explore vast space of materials efficiently (metals, oxides, nitrides, chalcogenides, ...)
Understand structure-property-function relationships
Predict reaction mechanisms and energetics/kinetics accurately

## Slide 13: Example: Using catalysts efficiently
Key Idea: Use minimal amount of Pt with tailored “supports” to get performance comparable to bulk Pt

## Slide 14: Example: Taking catalysts to the limit
Chen et al., Nature Nanotech 13, 702–707 (2018)
Zhang et al. ACS Nano 11, 6930-6941 (2017)
Yang et al., Science Advances 2 (2016)
Notes: Ru-graphene ORR catalysts

## Slide 15: Example: Designing Earth-abundant catalysts
Kuraganti, et al. ACS Appl. Mater. Interfaces 2019, 11, 28, 25155-25162
Ravikumar, H., et al. Materials Letters 220 (2018): 133-135
MoSe2 nanoflower
Dope edges with other transition-metal atoms

## Slide 16: DOPED MoSe2 ELECTROCATALYSTS
Strength of H binding increases
HER activity increases
Volcano plot (black dashed lines) from Esposito et al., J. Am. Chem. Soc., 2012, 134, 3025–3033.
BSL: Basal Plane
VSe: Se-vacancy
Doping is an effective strategy to activate MoSe2 for hydrogen production

## Slide 17: Beyond Hydrogen: Nitrogen Reduction
A. Jain, M. Bar Sadan, A. Ramasubramaniam
J. Phys. Chem. C, 125, 19980–19990 (2021)
H-mediated NRR:
N2 + 14 (H++e-)  2NH3 (g) + 4H2 (g)
NRR:
N2 + 6 (H++e-)  2NH3 (g)
Complex pathway involving coadsorbates, electrolyte effects, etc.
Plenty of ongoing research, a lot more to be done…

## Slide 18: Sourcing ‘PURE’ Water
Generating pure water is energy intensive

## Slide 19: Creating a Stable Water Catalyst
Smaller particles lead to a higher fraction
of exposed metal catalyst

## Slide 20: Focus topic: water electrolysis and PEM fuel cell experiment
Motor
Hydrogen Reservoir
Oxygen Reservoir
Fuel Cell
Energy Source

## Slide 21: Focus topic: water electrolysis and PEM fuel cell experiment
NIST.gov
PEM Fuel Cell
nafion.com
Recall Water Electrolysis: 2H2O (l)  2H2 (g)+ O2 (g)
Cathode: 4H+ + 4e-  2H2 (g)
Anode : 2H2O (l)  O2 (g)+ 4H+ + 4e-
Hydrogen Oxidation: 2H2O (l)  2H2 (g)+ O2 (g)
Anode: 4H+ + 4e-  2H2 (g)
Cathode : 2H2O (l)  O2 (g)+ 4H+ + 4e-
Running electrolysis in reverse

## Slide 22: Thank You!